Three THz metadevices: double-sided perfect absorber, miniature surface plasmon polariton amplitude modulator, and 3D negative index medium

Ta-Jen Yen,1,* Ting-Tso Yeh,1 Tsung-Yu Huang,1 Cheng-Wei Chang,1 Chu-En Lin,2 and Chih-Jen Yu3

1Department of Materials Science and Engineering, National Tsing Hua University, Hsinchu, Taiwan, R.O.C.

2Department of Mechanical Engineering, National Chin-Yi University of Technology, Taichung, Taiwan, R.O.C.

3Graduate Institute of Electro-Optical Engineering, Chang Gung University, Taoyuan, Taiwan, R.O.C.

*E-mail: tjyen@mx.nthu.edu.tw

In this talk, I introduce three metadevices: 1. A double-sided perfect absorber, 2. A miniature surface plasmon polariton amplitude modulator, and 3. A 3D negative index medium. Firstly, we design and demonstrate a flexible, ultrathin and double-sided metamaterial perfect absorber (MPA) at 2.39 terahertz (THz), which enables excellent light absorbance under incidences from two opposite sides. [1] Herein, the MPA is fabricated on a 0/10.1-thick flexible polyethylene terephthalate substrate of r = 2.75×(1+0.12𝑖), sandwiched by two identical randomized metallic patterns by our stochastic design process. Such an MPA provides tailored permittivity and permeability to approach the impedance of free space for minimizing reflectance and a great imaginary part of the refractive index for reducing transmittance and finally results in high absorbance. Both experimental measurement and numerical simulation are in a good agreement. The flexible, ultrathin and double-sided MPA significantly differs from traditional quarter-wavelength absorbers and other single-sided perfect absorbers, paving a way toward practical THz applications in thermal emission, sensing and imaging, communications, stealth technique, and even energy harvesting.

Next, we present a miniature surface plasmon polariton amplitude modulator (SPPAM) by directing and interfering surface plasmon polaritons on a nanofabricated chip. [2] Our results show that this SPPAM enables two kinds of modulations. The first kind of modulation is controlled by encoding angular-frequency difference from a Zeeman laser, with a beat frequency of 1.66 MHz; the second of modulation is validated by periodically varying the polarization states from a polarization generator, with rotation frequencies of 0.5-10k Hz. In addition, the normalized extinction ratio of our plasmonic structure reaches 100. Such miniaturized beat-frequency and polarization-controlled amplitude modulators open an avenue for the exploration of ultrasensitive nanosensors, nanocircuits, and other integrated nanophotonic devices.

Finally, we design and construct a three-dimensional (3D) negative index medium (NIM) composed of gold hemispherical shells to supplant an integration of a split-ring resonator and a discrete plasmonic wire for both negative permeability and permittivity at THz gap. [3] With the proposed highly symmetric gold hemispherical shells, the negative index is preserved at multiple incident angles ranging from 0° to 85° for both TE and TM waves, which is further evidenced by negative phase flows in animated field distributions and outweighs conventional fishnet structures with operating frequency shifts when varying incident angles. Finally, the fabrication of the gold hemispherical shells is facilitated via standard UV lithographic and isotropic wet etching processes and characterized by (-FTIR. The measurement results agree the simulated ones very well.

References

[1] Tsung-Yu Huang, Ching-Wei Tseng, Ting-Tso Yeh, Tien-Tien Yeh, Chih-Wei Luo, Tahsin Akalin, and Ta-Jen Yen, Scientific Reports 2015, 5, Article number: 18605

[2] Cheng-Wei Chang, Chu-En Lin, Chih-Jen Yu, Ting-Tso Yeh, Ta-Jen Yen, Scientific Reports 2016, 6, Article number: 32098

[3] Ting-Tso Yeh, Tsung-Yu Huang, and Ta-Jen Yen, Scientific Reports 2017, 7, Article number: 45549